Improvement of Motion Blur in Low Brightness and Grayscale of OLED Display Devices

Pan Wei*, Xiaoxu Hu*, Jun Lin*, Kai Zhu*, Zhenwei Han*, Hongyu Wang*, Mihwa Ha*, Wonjun Song*

* Kunshan Govisionox Optoelectronics Co., Ltd. (Visionox’s Affiliated Company), Kunshan, Jiangsu, P. R. China

Abstract

As the application scenarios of the active matrix organic light-emitting diode (AMOLED) products such as mobile phones and wearable devices increases, the motion blur in low-brightness and low-gray-scale is increasingly drawing the attention of consumers. Due to the D-TFT hysteresis effect of the organic light-emitting diode (OLED) devices and influence of organic light-emitting diode (OLED) capacitors, the brightness decreases at the first frame when the page scrolled, which cause a visually apparent in purplish red or other colors. In this work, various influencing factors of motion blur including OLED materials, capacitance, aperture ratio, horizontal crosstalk, data voltage setting and so on were systematically studied. Each factor improves the objective value by 1% to 10% respectively. The visual effect has improved from being noticeably purple to being almost invisible.

Author Keywords

Motion blur; low Brightness; capacitance; pixel aperture ratio; D-TFT stress; timing, data voltage.

Introduction

The active matrix organic light-emitting diode (AMOLED) products are widely applied in new display technologies, including mobile phones, wearable devices, laptops and televisions because of its low driving voltage, high contrast, wide color gamut, wide viewing angle, rapid response time, and low power consumption [1-2]. With the increase in low-brightness application scenarios, the low-brightness and low-gray-scale performance of the products such as image sticking, motion blur and color uniformity has drawn increasing attention from consumers.

A trailing phenomenon can be visually observed when we sliding the page of the product in low brightness, usually appears in a shade of purple, purplish red, blue or other colors. This is caused by the D-TFT hysteresis effect of the organic light-emitting diode (OLED) devices and influence of organic light-emitting diode (OLED) capacitors. When we switch the screen from black screen to low-brightness screen, for example 2nit, 5nit, or 5nit grayscale 128, different D-TFT stresses in the first frame and the subsequent frames, and the inconsistent initialization states of the organic light-emitting diode (OLED) anode, which results in a lower brightness in the first frame. The organic light-emitting diode (OLED) capacitance affects the length of the charging time. As we all know, white light is formed by combining the three primary colors of red, green and blue in a certain proportion, due to the inconsistent proportions of the low brightness levels of the three primary colors in the first frame, the above-mentioned color deviation in the first frame occurs when the page is scrolled. The OLED engineers have done a lot of work to improve the motion blur and make the color deviation invisible to the naked eye.

The first frame brightness ratio (FFR) is defined as: the brightness ratio between the first frame image and the steady-state image which is usually set to the maximum brightness of the first five frames when the screen transitions from a black screen to a grayscale screen. Traditionally, this ratio is calculated through analysis of the brightness waveform as shown in Figure1 and Equation (1). The expression method of the objective value for the motion blur evaluation is shown in Equation (2). Consumers are increasingly seeking to reduce the objective values.

Figure 1. Brightness waveform.

(1)

(2)

In this paper, we achieved satisfactory results in improving the motion blur not only by optimizing the structure using multiple components to reduce the capacitance differences among the three primary colors of the device, but also by reducing the lateral current leakage of the device and optimizing the driving settings of the device to reduce the influence of D-TFT stress.

Experimental

2.1 Device Fabrication: The wearable active matrix organic light-emitting diode (AMOLED) products was selected for validation. A conventional AMOLED process sequence has been employed for the fabrication of devices.

2.2 Testing Equipment: All samples were tested of the first frame brightness ratio (FFR) of the four color planes (W/R/G/B). The data were recorded with a CA410 (Konic Minolta, Inc., Tokyo, Japan).

Results and Discussions

3.1 Organic Light-emitting Diode (OLED) Material System: The selection of materials mainly depends on the mobility of the materials and their energy levels. It is possible to both control the size of the energy barrier between the device materials, ensuring that the device has good injection characteristics without generating a large amount of charge accumulation; and to set an appropriate difference in material mobility, so that there can be good hole transport capability between each layer of materials, without generating a large amount of space diffusion charges that increase the device capacitance.

Affected by the lighting voltage, efficiency and capacitance, products of different material systems showed significantly differences in motion blur performance. When selecting materials for device development, in response to the situation where the first frame brightness ratio (FFR) of each color in the previous material system were significantly different, targeted selection of materials was carried out to reduce the color with a high first frame brightness ratio (FFR) and increase the lower one, thereby achieving consistency in the first frame brightness ratio (FFR) of the three colors and improving the visual effect.

Table 1. Parameters for different material systems of Red @ 2nit.

| Parameters | System A | System B |
| --- | --- | --- |
| Von | 2.31 | 2.22 |
| Vd | 2.50 | 2.37 |
| Eff | 100% | +31% |
| Cp | 100% | +5% |
| FFR | 60.4% | 53.8% |

Due to the increase in capacitance of system B, the charging time to reach the target brightness getting longer, which results in a decrease in the first frame brightness ratio.

3.2 Optimization of Device Structure: The verification and mass production application of the new materials system take a relatively long time. The optimization of device structure offers greater advantages in mass production projects, and it can also play a role in regulating capacitance. The structural changes of the film layers cause variations in the energy barriers between adjacent film layers, and the location where charges accumulate in the device shifts, thereby resulting in differences in the device capacitance. Furthermore, changes in the thickness of the film layer can also serve to regulate the capacitance. This method is different from the adjustment of device structure, which may require the modification of the evaporation equipment. Instead, it can be achieved simply by adjusting the scan-time of the evaporation crucible, making the improvement method much easier and more convenient.

Figure 2. Capacitance of different device structures.

Figure 3. Capacitance of different thickness of the film layer.

Furthermore, due to the leakage current occurring at low brightness levels, the charge used for charging the capacitor decreases. Under the same capacitor size, the time required to fully charge is further prolonged, resulting in a reduction in the proportion of the first frame at low brightness levels. The differences in RGB leakage further exacerbate the incoordination of the brightness proportion of the first frame brightness ratio (FFR), leading to the occurrence of motion blur and color shift at low brightness levels. Therefore, optimizing the device structure and improving the leakage phenomenon is also an effective method for improving the low-brightness ghosting and color shift issues.

For instance, the first frame brightness ratio (FFR) of the green light is relatively low. Reducing the leakage current under low brightness conditions of the green light can effectively increase the charge quantity used for charging and thereby increase the first frame brightness ratio (FFR) of the green light. Usually, we use the spectrum to confirm the crosstalk and thereby determine the leakage current. As can be seen in Figure 4, the intensity of the red light spectrum near 630nm in the improved green light spectrum has decreased, indicating that the amount of charge leakage from green light to red light has significantly reduced. The verification results of 1.8X inch product show that the optimization of the device film thickness by 10 Å has led to an improvement in leakage, which has increased the proportion of the green light first frame brightness ratio (FFR) from 54% to 59%。

Figure 4. The green light spectrum before and after device optimization.

3.3 Optimization of Product Design: Whether it is the iteration of organic light-emitting diode (OLED) material systems or the optimization of device structures, what is changed is the capacitance per unit area. Product design optimization is achieved by adjusting the capacitance of individual pixels through changes in pixel aperture area. However, when the pixels per inch (PPI) is fixed, increasing the pixel aperture area will reduce the pixel pitch and increase defects during evaporation, such as color mixing resulting in color spots. Reducing the pixel aperture area will deteriorate the lifetime. The assessment data shows that a reduction of 1μm in pixel pitch lead to about 4% increase in related evaporation defect rate. The product verification results of the 1.7X inch product show that the pixel aperture ratio of the green light (with the lowest first frame brightness ratio (FFR)) has decreased by 1.22% (from 7.04% to 5.82%), the first frame brightness ratio (FFR) has increased by 4.6%, but the brightness lifetime of the green light T95 have decreased by 31%, and the brightness lifetime of the white light T95 have decreased nearly by 28%. Therefore, during the product development and design process, it is necessary to comprehensively evaluate the product's yield rate, lifetime and motion blur performance, in order to achieve a balance in performance.

Figure 5. Lifetime of different pixel aperture ratio of green light.

3.4 Optimization of D-TFT Stress: The D-TFT stress will exacerbate the drift of the D-TFT threshold voltage. For instance, under negative gate stress, the threshold voltage of the D-TFT will drift negatively, and the greater the stress, the more obvious the drift. This drift will further amplify the lag effect, resulting in insufficient brightness in the first frame, especially more prominent in low-brightness scenarios. Therefore, through process optimization, improving the D-TFT stress is also an important direction for improving motion blur.

Figure 6. The first frame brightness ratio (FFR) under different DOE conditions.

By comparing the first frame brightness ratio (FFR) and process monitoring data under different DOE conditions, it can be observed that D-TFT Vth is directly related to the first frame brightness ratio (FFR) under low brightness conditions. This is because Vth is negatively biased, and after VGMP is written to Cst, the Gate level is low, thereby weakening the stress of D-TFT under the black state of VGMP, resulting in a significant improvement in the first frame brightness ratio (FFR) under low brightness conditions.

Table 2. Vth for different DOE conditions.

| Conditions | Vth | FFR |
| --- | --- | --- |
| DOE1 | -1.40V | 50.8% |
| DOE2 | -2.44V | 65.9% |
| DOE3 | -1.26V | 44.8% |

3.5 Optimization of Timing and Data Voltage: The verification results show that increasing the Scan frequency of Timing can significantly improve the first frame brightness ratio (FFR) of W/R/G/B at low brightness levels. The main reason is that compared to 1Scan, 2Scan optimizes the scanning method and driving Timing, adds 1 pre-initialization and write to refresh the D-TFT stress state, allowing the characteristics to recover, effectively reducing the hysteresis effect of D-TFT and pixel response delay. After verification, for the same product, under the same design and process conditions, changing the Scan frequency alone, △R/G/B value of 2Scan is reduced by approximately 5% compared to 1Scan, and 3Scan is reduced by approximately 15% compared to 1Scan. As seen in Figure7, the first frame brightness ratio (FFR) in 2Scan not only has a shorter activation time but also has significantly higher brightness, which indicates better performance in motion blur.

Figure 7. Comparison of brightness waveforms of different scan Timing.

The VGMP voltage is the maximum voltage set by the module code, which enables the screen to display a black image. The voltage that can precisely make the screen display a black image is called the black state voltage. The VGMP usually requires a voltage level that is greater than or equal to the black state voltage. The higher the VGMP voltage setting of the module code, the lower the first frame brightness ratio (FFR). And as the brightness decreases, the influence of the VGMP settings on first frame brightness ratio (FFR) gradually increases.

Figure 8. The first frame brightness ratio (FFR) for different VGMP voltage settings (voltage represents the black state voltage in the figure).

Figure 9. The first frame brightness ratio (FFR) of different brightness for different VGMP voltage settings (voltage represents the black state voltage in the figure).

Differentiating the VGMP voltage of R/G/B can achieve the differentiation of D-TFT stress and Vd voltage, enabling the first frame differential charging rate of R/G/B when transitioning from black screen to grayscale screen. This way, it reduces the first frame brightness ratio (FFR) difference of R/G/B, thereby achieving the goal of improving motion blur and color shift.

Under the specified brightness specifications, by combining the curves of different VGMP voltages and the first frame brightness ratio (FFR) of R/G/B, and making differentiated selections of the VGMP voltages, it is possible to effectively reduce the objective value of the motion blur evaluation. For example, when the normal VGMP voltage is set to 5.5V, the first frame brightness ratio (FFR) of red under 2nit W255 is approximately 69%. According to the curve of the G/B VGMP and the first frame brightness ratio (FFR) under this brightness, the VGMP voltage of Green should be set to the black state voltage +0.2V and the VGMP voltage of Blue should be set to the black state voltage +0.45V.

Figure 9. The first frame brightness ratio (FFR) of G/B for different VGMP voltage settings (voltage represents the black state voltage in the figure).

Additionally, in order to prevent the VGMP setting from being too low, which could lead to the occurrence of dark crush anomalies after the reliability verification process, we carried out a series of reliability tests for 240 h, including high temperature operation (HTO) at 70℃, high temperature storage (HTS) at 80℃, low temperature operation (LTO) at -20℃, low temperature storage (LTS) at -40℃, 60℃ +90% humidity operation, 60℃ +90% humidity storage, 85℃ +85% humidity operation, 85℃ +85% humidity storage and thermal shock for 100 cycle, one cycle consists of -40℃ maintained for 30 minutes, 80℃ maintained for another 30 minutes, and the temperature change completed within 5 minutes. The improved product did not exhibit any abnormalities.

Conclusions

In this paper, we introduced our effective method in improving motion blur. Through the iteration of organic light-emitting diode (OLED) material systems, device structures optimization, process optimization and timing and data voltage optimization, the objective value of the motion blur was ultimately effectively reduced to 9%, and the visual effect of the products was significantly improved to imperceptible to the naked eye. Meanwhile, the products are comparable in other performance characteristics before and after improvement.

b

a

Figure 10. Comparison of visual effects before (a) and after (b) improvement.

As the application scenarios of the products become increasingly diverse and the application brightness decreases, solutions for the improvement of motion blur at lower brightness levels requires continuous exploration by all of us.

Acknowledgement

We want to acknowledge the Kunshan Govisionox Optoelectronics Co., Ltd. and Visionox Technology Co., Ltd. who provided an excellent platform for theoretical guidance, material preparation, financial and technical support. And we are grateful for efforts from all colleagues.

References

- Huang Y, Hsiang E L, Deng M Y, et al. Mini-LED, Micro-LED and OLED displays: present status and future perspectives[J]. Light: Science & Applications, 2020, 9(1):105

- Song J, Lee H, Jeong E G, et al. Organic light-emitting diodes: pushing toward the limits and beyond[J]. Advanced Materials, 2020, 32(35): 1907539.