A Study on Low-Brightness Uniformity in AMOLED Displays under Global DC Dimming: Challenges, Modeling, Mitigation

Xinquan Chen, Huiming Wang, Wenquan Chu, Ke Liu, Weibin Zhang, Ran Chen, Ying Shen

*Hefei Visionox Technology Co.,Ltd. Hefei, China

Abstract

An improved model and solution framework are proposed to address Global DC low-brightness mura by optimizing the Thin-Film Transistor sub-threshold swing and advancing Demura compensation technology. Experimental validation demonstrates that the proposed approach achieves over 35% improvement in reducing color non-uniformity (ΔE).

Author Keywords

Global DC Low-Brightness mura; sub-threshold swing; Demura compensation; color non-uniformity (ΔE)

Introduction of Global DC Dimming

Conventional hybrid DC + PWM dimming, as illustrated in Figure 1, controls the on/off time of pixels by adjusting the duty cycle (number of pulses) of the GIP EM signal during low-brightness display on OLED panels. This approach achieves regulation over the pixel current and instantaneous luminance while maintaining the effective visual brightness of the screen. Consequently, it can circumvent issues such as Mura deterioration and insufficient precision of the IC data voltage output, which arise when OLED pixels enter the low-current operation region.

EM(DC)

EM(PWM)

EM(Global DC)

Figure 1.  hybrid DC + PWM dimming

Figure 2.  Global DC dimming

This study investigates a global DC dimming mode, depicted in Figure 2. Its characteristic is that across the entire brightness range from low to high, the EM duty cycle and EM pulse remain constant for the OLED panel, with the number of pulses fixed at one—an extreme scenario. Dimming is achieved solely by modulating the data voltage output from the driving IC, which controls the TFT current and thereby regulates the current flowing through the OLED pixel. Research indicates that this mode more closely mimics natural light, offering potential benefits for enhancing the user viewing experience and promoting eye health.

As mentioned, since global DC dimming represents an extreme operational scenario for OLEDs, apart from benefits like reduced eye strain, it also presents significant challenges. This mode makes the display more susceptible to operating in the TFT low-current region at low brightness levels. Furthermore, when combined with advancements such as iterations in EL materials, COE technology, and tandem architectures, it tends to amplify inherent defects in the TFT fabrication process. This exacerbates various types of optical non-uniformity visible to the human eye, thereby imposing more stringent requirements on the TFT manufacturing process.

Global DC Dimming: Navigating Challenges in Low-Brightness Environments

2.1 Impact on TFT Process and Current Requirements

In a global DC dimming scenario, the transient current flowing through the OLED pixel can be reduced by more than 50%. Separate analysis of the efficiency gains from the iteration speed of current EL materials, the efficiency benefits of COE technology, and the efficiency benefits of tandem technology reveals that they can bring at least 30% and 20% power savings respectively. This implies that iterations in EL materials, COE technology, and tandem technology can respectively bring at least equivalent efficiency improvements. Correspondingly, this means a reduction in the transient current cost through the OLED pixel. If global DC dimming is fully combined with these technologies, a current reduction of at least 70% can be achieved. This change in the operational scenario will multiplicatively increase the challenges for the TFT fabrication process. This is precisely the core reason why Global DC technology has not been successfully commercialized in OLEDs since mass production began. As TFT process capabilities improve and external compensation techniques advance, this application scenario becomes more feasible and is once again being seriously considered.

Table1. OLED Current Reduction Achieved by Different Technical Solutions

| New Technology/Process | OLED Current Reduction |
| --- | --- |
| OLED Material Iteration | Reduced by 10% |
| COE​ | Reduced by 30% |
| Tandem​ | Reduced by 20% |
| Global DC Dimming) | Reduced by 50% |

2.2 Increased Sensitivity in the Sub-threshold Region and Mura Deterioration

The drain-source current (Ids) is dominated by the diffusion mechanism. When the gate voltage changes minutely, the current fluctuation becomes significant. As shown in Figure 3, as the OLED current (Ioled) decreases, the sensitivity of the driving TFT (DTFT) impedance increases, and process non-uniformity is amplified. Consequently, intra-panel and inter-panel display variations worsen, primarily manifested as a deterioration in ΔE (luminance and color non-uniformity). As shown in Figure 4, specific manifestations include degraded color uniformity, more severe Mura, and Dirty Mura that is more difficult to overcome.

Figure 3. Explanation of TFT Sub-threshold Region & Current Sensitivity.

Figure 4. Images demonstrating worsened color non-uniformity (ΔE) and Mura.

2.3 Increased Demand for Driving IC Voltage Output Precision

At low brightness levels, taking 2 nits as an example, unfolding 255 grayscale levels under 2 nits requires high precision. Since only the data voltage controls the brightness, the voltage difference between grayscale 255 and grayscale 0 at 2 nits is small, demanding a more refined grayscale unfolding voltage. This places higher requirements on the output precision of the Display Driver IC (DDIC). As shown in Figure 5, comparing the required voltage precision for grayscale unfolding at 2 nits: PWM dimming requires 0.0076 V, while global DC dimming requires 0.0027 V—the precision requirement is approximately twice as high.

Figure 5. Required voltage precision for panel grayscale unfolding.

2.4 Experimental Validation of Performance Deterioration

Based on the theoretical analysis above, the main impacts of low-brightness DC dimming on display performance were identified. Practical validation was conducted on a specific project comparing hybrid dimming and global DC dimming. The results, shown in Table 2, indicate that the maximum color non-uniformity (ΔE max) at 32 grayscale and 2 nits worsened from 49.29 to 79.36 when using global DC dimming. Without optimization of the TFT process and compensation algorithms, this represents a 74.5% deterioration. Other types of Mura showed similar or even more severe worsening trends.

Table 2: Comparison of display performance parameters (ΔE max, etc.) between hybrid dimming and global DC dimming at low brightness(32pcs).

| ITEM | PWM | DC |
| --- | --- | --- |
| Delta Ex | 49.29 | 79.36 |

Analysis of Influencing Factors and Optimization Schemes for Global DC Dimming at Low Brightness

3.1 Operational Characteristics in the Sub-threshold Region

When the Driving Thin-Film Transistor (DTFT) operates in the sub-threshold region, the DTFT is in a weak inversion state near the interface. The drain-source current (Ids) is dominated by the diffusion mechanism. On a logarithmic scale, Ids exhibits a linear relationship with the gate-source voltage (Vgs). The current formula for the sub-threshold region is as follows:

Parameter Description:

IDS: Drain-source current (Unit: A)

I₀: Saturation current (related to material properties and interface state density)

VGS: Gate-source voltage (Unit: V)

VTH: Threshold voltage (Unit: V)

VT​ (Thermal voltage): VT = kT/q ≈ 26 mV (at room temperature)

n: Subthreshold swing coefficient, typically n ≥ 1. It is influenced by interface state density and mobility, and in TFTs, n is often greater than 1 (e.g., n=2).

S.S.​ (Subthreshold Swing): S.S. = n • VT • ln(10). The subthreshold swing refers to the change in gate voltage required to alter the drain current by one order of magnitude in the sub-threshold region. An increase in S.S. means a larger voltage change is required to vary the current by one order of magnitude (corresponding to a change in grayscale). This can enhance current stability and improve luminance uniformity.

3.2 Proposed Optimization Strategies

Based on the above analysis and modeling, this paper proposes the following optimization strategies:

(a)DTFT Long-Range and Short-Range Uniformity Optimization:  Improve the uniformity of parameters such as VTH, gate insulator (GI) interface quality, and S.S. through process and material adjustments. This aims to optimize various Mura types (e.g., LENS Mura, ELA Mura, Oven Mura, spot Mura), thereby improving ΔE. Based on mass production data, this approach can contribute to a 10% to 20% improvement in ΔE.

(b)Zoned S.S. (Subthreshold Swing):The theoretical analysis easily leads to the conclusion that increasing the S.S. can effectively mitigate the impacts of low current at low brightness. However, the associated negative effects are also significant, such as an increase in the data voltage required for black state and varying degrees of impact on short-term image sticking, smearing, and crosstalk. Clearly, to improve image quality in the Global DC low-current mode, optimizing the TFT cannot simply rely on a brute-force, single-minded increase of the S.S. The ideal scenario, considering OLED image quality requirements and current challenges, is to achieve a TFT with an IDS-VGS characteristic featuring a small S.S. in the high-current region and a large S.S. in the low-current region. Based on this analysis, a zoned S.S. model is proposed and practiced.

Figure 6. introduction of Zoned S.S. (Subthreshold Swing)

As shown in Figure 6, the gate voltage difference corresponding to the DTFT's IDS change from 10nA to 100nA is defined as DR1. A smaller DR1 indicates a larger slope in this region, leading to more sufficient data writing and better VTH compensation capability. The resulting product performance includes a lower data voltage and reduced Mura caused by VTH fluctuation. Therefore, DR1 should be minimized.

The transient current of the DTFT in a 2nit L32 image is approximately 40pA. The gate voltage difference corresponding to the IDS change from 10pA to 100pA in the DTFT's IDS-VGS curve is defined as DR2. A larger DR2 indicates a smaller slope in this region, making grayscale expansion easier and improving low grayscale image quality.

This paper proposes a zoned S.S. scheme. By controlling the S.S. magnitude in different segments, it optimizes both low-brightness grayscale expansion (γ) and ensures data charging rate (affecting data voltage and compensation capability) at higher brightness levels, as illustrated in Figure 6.

Data indicates a clear linear relationship between DR2 and the voltage required for grayscale expansion, as shown in Figure 7. A larger DR2 increases the required grayscale expansion voltage margin from the driver IC, thereby optimizing Mura. The zoned S.S. strategy contributes up to a 10% improvement in ΔE.

Figure 7. Data relationship between DR2 and the voltage required for grayscale expansion

(c)Multi Demura: A production engineering technology named Multi Demura has been developed, integrating AI module position recognition, AI Mura pattern detection, and adaptive demura algorithm matching. It aims to maximize display quality improvement in complex scenarios characterized by diverse Mura types and varying severity levels, while also balancing production capacity and the inherent characteristics of the OLED product. It can be categorized into low-tier and high-tier Multi Demura routes. The core difference lies in how they balance the degree of Mura improvement against the impact on associated production tact time (TTF).

The low-tier Multi Demura scheme combines AI module position recognition with demura algorithms and adapts local secondary demura technology based on the product's TFT short-range performance. The high-tier Multi Demura scheme, in addition to the technologies in the low-tier scheme, incorporates AI Mura pattern technology and a complete set of secondary and multiple demura technologies, contributing over 20% to ΔE improvement. However, the high-tier scheme also has significant drawbacks: if implemented on existing production lines, the impact on the module production line would require substantial cost investment.

Figure 8. AI Demura compensation effect.

(d)Differentiated VGSP(gamma low voltage) Setting

This strategy involves dynamically setting the VGSP voltage. Specifically, raising the VGSP in the low-brightness band makes the gamma voltage change less for the same register value, thereby increasing gamma voltage precision. This improves low-brightness grayscale expansion, optimizes Mura performance, and enhances Demura compensation capability. This scheme has already been implemented in projects.

Furthermore, raising the low-brightness V<sub>GSP</sub> voltage significantly optimizes the precision of the grayscale expansion voltage. Verification results, as shown in Figure 9, indicate that when V<sub>GSP</sub> is raised to 2.8V, it well matches the source driver voltage precision requirements for low-brightness DC dimming.

Figure 9. Validation data for differentiated VGSP settings.

Optimization Results of Global DC Dimming

By integrating the zoned S.S. TFT process technology, AI-powered Multi-Demura, and optimized driver IC solutions under the global DC dimming mode, the key metric for display uniformity—the color difference (ΔE) at low brightness—can be effectively reduced by over 35%. Concurrently, the gamma (γ) convergence at 2 nits is also improved.

Furthermore, the optical performance of the global DC-based product is enhanced. It achieves flicker-free or low-flicker states, with performance characteristics consistent with those of hybrid dimming modes. The technology has now reached a level ready for mass production.

Conclusion

This paper has proposed a comprehensive set of optimization solutions focused on improving ΔE. The core developments include a zoned Sub-threshold Swing (S.S.) TFT process technology and advanced Multi-Demura compensation techniques (encompassing both high-tier and low-tier schemes incorporating AI module recognition). Validation data from mass production indicates that the implementation of these solutions effectively mitigates the display quality degradation associated with global DC dimming, achieving a remarkable improvement exceeding 35% in ΔE. This progress paves the way for the successful mass production adoption of full-range DC dimming technology

References

- L. Gong, Z. Tang, Z. Chen, et al. "Sub-second Long Lifetime Triplet Exciton Reservoir as Assistant Host for Highly Efficient and Stable Organic Light-Emitting Diode." Advanced Functional Materials, Early View, March 2025.

- L. Wu, Z. Xin, D. Liu, et al. "Bifunctional Group Modulation Strategy Enables MR‐TADF Electroluminescence Toward BT.2020 Green Light Standard." Advanced Materials, 2025, 2416224.

- Zhou, X., Zhu, S., Zhou, T., & Chen, C. (2025). P‐14.23: Design of oxide TFT adaptive device based on OLED. SID Symposium Digest of Technical Papers, 56(S1), 1757–1759. https://doi.org/10.1002/sdtp.19206