Sparkle Optimization in Display Modules with Anti-Glare Cover Glass

Endong Chang*, Jiuhui Zhang*, Shuai He*,Peng Cheng*, Tongmin Liu*

* Hefei Govisionox Technology Co., Ltd., Hefei, Anhui, China

Abstract

This study summarizes the influence laws of three typical AG processes (photolithography process, frosting etching process, and abrasive blasting process) on the microstructure and sparkle characteristics. On this basis, by introducing a light diffusion film into the display module and combining it with the frosting etching process to fabricate the AG cover glass, the sparkle issue is effectively improved.

Author Keywords

OLED module; cover glass; AG(anti-glare); Sparkle

The impact of AG treatment on the cover glass

The development of information technology has driven the evolution of display technologies toward thinness, high image quality, and superior user experience. Organic Light-Emitting Diodes (OLED), leveraging advantages such as self-illumination, high contrast, wide viewing angles, and flexible foldability, have become a mainstream technology in fields like smartphones and in-vehicle displays. The global OLED market scale continues to grow, demonstrating significant development potential.

However, OLED are prone to glare under strong outdoor light or complex indoor lighting conditions, which reduces display clarity, causes eye fatigue, and impairs user experience. The industry commonly adopts Anti-Glare (AG) covers to address this issue. As shown in Figure 1 and Figure 2, The micro-nano rough structure on the surface of AG covers converts specular reflection into diffuse reflection, effectively reducing glare. AG covers have thus become a key component in OLED production.

Nevertheless, As shown in Figure 3, AG covers introduce a "spark"—under specific lighting, uneven micro-nano structures, material properties, and manufacturing processes lead to localized abnormal brightness elevation on the surface. This disrupts display uniformity, particularly in dark images or low-light environments. As user demands for display quality increase, the sparkle issue restricts the application of AG covers and has attracted attention from academia and industry. Based on this, this paper focuses on the spark issue of AG covers for OLED screens, aiming to provide references for solving this technical challenge.

Figure 1. Schematic diagram of AG cover glass with glare microstructure

Figure 2. Comparison of anti-glare properties between AG cover glass and non AG cover glass (left shows AG treated, right shows untreated) and scanning electron microscope images of AG cover glass surface

Figure 3. Schematic diagram of spark generation of AG

Different strategies to reduce Sparkle

Table 1. The influence of different CG processes on performance parameters and surface structure

| - AG Technology | - Performance(254ppi) | - Micrograph | - Laser 3D image | - Particle size distribution and concave depth | - Instructions |
| --- | --- | --- | --- | --- | --- |
| - Photolithography | - Haze：40.6% - Ra:0.504um - Gloss:19.9 - Sparkle:3.0 |  |  | - 22~30μm/5~6μm | - Pentagonal, with arches on all sides and a depression in the middle. The size differences between units are small and evenly. - Good spark effect |
| - Frosting etching | - Haze：44% - Ra：0.423um - Gloss：21 - Sparkle：8.2 |  |  | - 8~22μm/2~7μm | - The structure is amorphous (close to circular) with arches on all sides and a depression in the middle, with varying sizes. The higher the haze, the larger the structure size, but the depth difference is not significant; The lower the haze, the smaller the sparkle. The sparkle of photolithography AG is due to frosting etching AG |
|  | - Haze：30% - Ra：0.261um - Gloss：21.5 - Sparkle：5.2 |  |  | - 7~12μm/1~4μm |  |
|  | - Haze：20.4% - Ra：0.239um - Gloss：28.6 - Sparkle：4.1 |  |  | - 5~12μm/2~5μm |  |
| - Abrasive blasting | - NA |  |  | - 5~10μm/2~3μm | - The structure is a circular pit with arches on all sides and a depression in the middle, with a relatively uniform size distribution (between frosting etching and photolithography) |

- 3.  Impact and Outlook

Aiming at the sparkle issue of AG anti-glare covers for displays, as shown in Figure 4 and Figure 5,this work introduces a light-diffusion film into the display module and applies the AG Frosting etching process to the cover. As shown in Table 2, The optimized module achieves both high haze and low sparkle, solving the long-standing conflict between AG anti-glare performance and sparkle defects. It expands AG covers’ application in in-vehicle and medium-sized displays—ensuring clear in-vehicle display under complex lighting and enhancing user comfort for medium-sized devices, supporting display product upgrades.

In this study, an etched frosted AG cover plate was adopted as the substrate, and a Light Diffusion Film was integrated between the Polarizer (Pol) and Cover Glass (CG) of the display module. Four types of LDF with distinct pitch parameters were prepared, namely 5 μm pitch, 2 μm pitch, and two 8 μm pitch variants, all of which were laminated with the identical AG cover plate and display panel for parallel testing.

This work adopted the SMS1000 device to test the sparkle value of the green light image (because the human eye is more sensitive to green light) and conducted a subjective evaluation combined with the sparkle effect.

Figure 4. frosting etching process AG Process Flow Diagram

Table 2. Sparkle and haze performance indicators of different test samples (3A cover glass and 3A cover glass with 5μm pitch Light Diffusion Film) (3A refers to anti finger, anti glass, anti reflex)

| Split | CG(3A) | CG(3A) with LDF Sparkle Improvement Ratio | Specifications |
| --- | --- | --- | --- |
| 1# | 5.33-5.85 | ~67% | Haze20% Ra0.25μm |
| 2# | 4.59-5.01 | ~69% | Haze30% Ra0.25μm |
| 3# | 5.81-6.30 | ~63% | Haze30% Ra0.35μm |
| 4# | 4.51-5.01 | ~61% | Haze40% Ra0.35μm |
| Visual Effect | Severe Sparkle | Imperceptible(<3) | / |

Figure 5. Schematic diagram of AG cover glass with uniform light film added to reduce sparkle principle

Figure 6. Optical Model of OLED Module Stack with LDF[1]

As shown in Figure 6, each sub-pixel in the OLED light-emitting layer forms multiple images after grating diffraction through the Light Diffusion Film (LDF). There is a lateral displacement dx between these images, where D is the optical path from the pixel layer to the LDF.[2] It is obtained by multiplying the physical distance d between the LDF and the pixels by the refractive index n .

dx=D∙tanθm                                   (1)

θm​is the m-th order diffraction angle, with λ is the wavelength,

T is the grating period, and m is the diffraction order.[3] which can be given by the following equation:

sinθm=mλT                                   (2)

Since most of the light is concentrated on the diffraction orders of 0 and ±1, only the cases of m=0 and ±1 are considered. [4]For normal light incidence and small diffraction angle θm, |m|=1, the calculation formula of the grating period T is as follows:

T=λnddx                                        (3)

When the sub-pixel gap is completely matched with the grating period, the sparkle can be reduced to the minimum. According to the OLED pixel design scheme, when the lateral displacement dx is approximately equal to 1/3 of the pixel pitch, the sub-pixel gap can be completely filled, which is the ideal state. Theoretically, the optimal grating period of the LDF is correlated with the distance from the LDF to the pixel layer: the larger the grating period, the larger the corresponding distance to the display pixel layer is required. With the improvement of display pixel density nowadays, the pixel size will gradually decrease. At this time, it is necessary to reduce the distance between the LDF and the display pixels, or increase the grating period of the LDF.

As shown in Table 2, It can be seen that: 1) Without the LDF, the sparkle values of Split 2 and Split 3 indicating that under the same haze condition, the higher the cover glass roughness, the more severe the sparkle; the sparkle of Split 3 and Split 4 indicating that under the same roughness condition, the lower the cover glass haze, the more severe the sparkle. 2) With the LDF, the sparkle of all schemes is significantly improved. Among them, Scheme 2 with a cover glass of 30% haze and 0.25μm roughness has the lowest sparkle value.

Table 3. The impact of different LDFs on Sparkle

| Split | 1# | 2# | 3# | 4# |
| --- | --- | --- | --- | --- |
| Grating Type | Rectangle | Rectangle | Sinusoidal | Sinusoidal |
| Process | UV Alignment | UV Alignment | Mold embossing | Mold embossing |
| T(pitch) | 5μm | 2μm | 8μm | 8μm |
| Sparkle | 2.39 | 2.34 | 3.40 | 3.60 |
| Haze | 87% | 78% | 54% | 34% |
| Visual Evaluation | Slight Sparkle | Slight Sparkle | Serious Sparkle | Serious Sparkle |

As shown in Table 3, the impact of different LDF designs on the sparkle effect of AG cover glass was systematically evaluated. The 1# and 2# samples, which employed rectangular gratings with 5μm and 2μm pitches respectively and were fabricated via UV alignment, exhibited relatively low sparkle values of 2.39% and 2.34%, accompanied by haze levels of 87% and 78%, and were rated as having "Slight Sparkle" in visual evaluation; additionally, LDFs prepared by UV alignment technology pose no risk of moiré patterns. In contrast, the 3# and 4# samples, featuring sinusoidal gratings with an 8μm pitch and produced by mold embossing, showed significantly higher sparkle values of 3.40% and 3.60%, with lower haze levels of 54% and 34%, respectively, and were assessed as having "Serious Sparkle"; it is noteworthy that LDFs manufactured by mold embossing processes carry a risk of moiré patterns, thus requiring the definition of die-cutting angles during practical application to mitigate this issue. These results indicate that smaller grating pitches (2μm and 5μm) combined with UV alignment technology can effectively suppress the sparkle phenomenon while avoiding moiré pattern risks, whereas larger pitches (8μm) and mold embossing processes lead to more severe sparkle issues and potential moiré pattern hazards. Notably, the 2# sample (2μm rectangular grating, UV alignment) demonstrated the optimal performance, achieving the lowest sparkle level (2.34%) with moderate haze, making it a promising candidate for balancing anti-glare performance and visual quality in display applications.

As shown in Figure4. This flowchart (Figure 4) illustrates the complete frosting etching process for the fabrication of AG (Anti-Glare) cover plates In the pre-treatment stage, the process initiates with raw material cutting and cleaning, followed by printing clearance holes and laminating an acid-resistant protective film to shield specific areas from etching. The core etching stage involves film pressing for adhesion reinforcement, loading the substrates, and pre-frosting cleaning before the critical frosting etching step. In the post-processing stage, the etched substrates undergo post-frosting cleaning to remove chemical residues, followed by liquid polishing to optimize surface quality. The process concludes with unloading the finished substrates and conducting comprehensive parameter measurement to verify the AG performance meets the technical specifications.

To further summarize the core characteristics of the three AG processes: Frosting etching AG has mature technology and low cost, but its surface structure is disordered (nearly circular), with poor uniformity of particle size and height, and weak sparkle control ability. Although photolithography AG has higher cost, relies on Mask design (to avoid moiré patterns) and its technology is not yet mature, it has an ordered surface structure (pentagonal) with high uniformity of particle size and height. It can effectively avoid the trade-off effect of frosting etching AG and is a key optimization direction for reducing sparkle. Abrasive blasting AG has an ordered surface structure (circular), with moderate uniformity of particle size and height (between frosting etching and photolithography AG), but high process.

Future research can adopt Micro-Lens Array (MLA) technology to address AG cover sparkle. As shown in Figure 6. by combining high and low refractive index materials in MLA, light can be enhanced or weakened at specific spatial angles, enabling orderly spatial light field distribution and efficient anti-glare. This solution suits extreme environments (e.g., ultra-bright outdoor displays) and high-end fields like medical monitors. Future work may focus on optimizing MLA material ratio, improving manufacturing precision, and integrating MLA with display modules.

Figure 7. Schematic diagram of Micro-Lens Array OLED

- References

- Cheng, P., Liu, R., Qiao, G., Ge, M. and Shen, Y. (2025), 68-2: Impact of Light -Diffusion Film on the Sparkle of OLED Display. SID Symposium Digest of Technical Papers, 56: 925-927. https://doi.org/10.1002/sdtp.18321

- Becker, M. E.  (2016): Late News Paper: Sparkle Evaluation with Visual Weighting. SID Symposium Digest of Technical Papers, 47(1).

- Valeriano, Ferreras, Paz, et al(2018). Sparkle Characterization of Anti-glare Layers on Displays with a Grey Value Histogram Analysis. SID International Symposium: Digest of Technology Papers, 49(1):76-79.

- Moharam, M. G., & Gaylord, T. K. (1982). Diffraction analysis of dielectric surface-relief gratings. Journal of the Optical Society of America, 72(10).