Investigation of Water Resistance in Monolithic AMOLED Modules

Rukang Zhang*, Luna Wang**, Ying Cao**, Gaohui Xie**, Mingwei Ge**, Ying Shen**

*Guangzhou Govisionox Technology Co., Ltd. (Visionox's Affiliated Company), Guangzhou, Guangdong, China

**Guangzhou Govisionox Technology Co., Ltd. (Visionox's Affiliated Company), Guangzhou, Guangdong, China

Abstract

Driven by increasing consumer demand for water resistance in the consumer electronics sector, particularly in mobile phones, the waterproof performance of AMOLED modules-as a key component of smartphones-has gained significant attention from device manufacturers. This study systematically analyzes the structural design and manufacturing processes of AMOLED modules. To address waterproofing requirements, we redesigned the sealing structures at critical locations, including the outermost area of the Flexible Printed Circuit (FPC), as well as the electrical connection interfaces such as FOP (FPC on Panel) and COP (Chip on Panel). Furthermore, the IPX8 waterproof test standard was deconstructed and adapted into a test method suitable for individual modules. Design of Experiments (DOE) results demonstrate that only well-designed waterproof pathways combined with strict control of module assembly processes can ensure that the waterproof performance of AMOLED modules meets customer expectations.

Author Keywords

AMOLED; Waterproof; COP; FOP

1. Introduction

In today's highly competitive smartphone market, user expectations regarding device reliability have become increasingly stringent. Requirements for dust and water resistance have evolved from IP67 to IP68 and IP69, reflecting a trend toward higher overall device protection ratings. At the same time, narrow bezels and high screen-to-body ratios have become major selling points for flagship models. However, the pursuit of ultra-narrow borders and maximized display area conflicts with the need for robust waterproofing. As smartphone screen bezels continue to shrink and Cover Glass (CG) ink borders are progressively narrowed, the sealing and dispensing process for the device mid-frame faces growing challenges, ultimately affecting the overall waterproof integrity. To resolve this technical conflict, extensive research has been conducted on mid-frame dispensing techniques, leading to the development of advanced encapsulation technologies such as Low Injection Pressure Overmolding (LIPO) [1]. In parallel, device manufacturers have shifted part of the waterproofing responsibility to display suppliers, imposing stricter requirements on the waterproof design and manufacturing processes of individual OLED modules. Key challenges now include how to implement effective waterproof structures at the module level, how to control process capability during production, and how to characterize and test the waterproof performance of standalone modules. This paper investigates these aspects by focusing on test methods for AMOLED module waterproofing, structural design strategies, and assembly process optimization.

2. Waterproof Design and Post-Test Dissection Evaluation of Module Units

Through investigation into the structural design and manufacturing process of the module unit, the key influencing factors for module waterproofing have been deconstructed, as summarized in Table 1.

Table 1. Key Influencing Factors for AMOLED Unit Waterproofing

| Item | Location | Key Influencing Factors |
| --- | --- | --- |
| Primary Influencing Factor | Outermost waterproofing | Waterproofing adhesive between the insulating tape, panel, and FPC |
|  |  | Waterproof path of the FPC backside adhesive |
|  |  | Bonding integrity between the support film and the spacer block |
|  |  | Bonding integrity between the spacer block and the SCF |
| Secondary Influencing Factor | Electrical connection points | FOP front-side adhesive (UV) |
|  |  | FOP back-side adhesive (UV) |
|  |  | DDIC encapsulation (UV) |
|  |  | Encapsulation of components such as TPIC, DDIC, capacitors, and resistors |

Component-level Waterproof Design to achieve effective waterproof design for the module unit, it is necessary to deconstruct and design individual components. The configuration of a module in the FOP (FPC on Panel) state is shown in the figure 1 below.

Figure1. State diagram of FOP modules

Waterproof Design of FPC Units: The adhesive application path and width design for the backside adhesive between the FPC and the SCF copper foil surface can be designed as a rectangular(口-shaped) adhesive structure, as shown in Figure 2. Potting treatment should be applied to electronic components (e.g., capacitors, resistors) on the FPC, as shown in Figure3. Particular attention must be paid to the width and height of the waterproof adhesive applied over the components.

Figure 2 ."口"-shaped backside adhesive application for FPC

Figure 3. Schematic diagram of component potting

Potting Treatment for Critical Electrical Connection Areas: After COP and D-IC bonding UV potting should be applied around the IC to prevent moisture ingress into the ACF connecting the IC to the panel or into exposed metal areas, which could cause electrical connection failures. The required potting width and height [2] for the D-IC are shown in Figure 4.For the FOP location, both the front and back sides must be coated with a layer of UV-curable resin (commonly referred to as front-side UV adhesive and back-side UV adhesive). The front-side adhesive must completely cover the FPC gold fingers and the panel signal connection pins, fully filling the height difference between the FPC and the panel. The back-side adhesive must completely cover the step differences between the FPC, the panel, and the support film. This prevents moisture from entering from the front or back of the FOP, which could cause water-oxygen corrosion on the FPC pins and the panel signal pins. A schematic cross-sectional view of the local area after COP potting, FOP front/back adhesive application, pad bending, and insulation tape attachment is shown in Figure 5.

Figure 4. Schematic diagram of D-IC sealing

Figure 5. Schematic diagram of adhesive application for FOP and COP sealing.

The primary key factor for waterproofing: the design of the FPC adhesive. The adhesive is applied to the flexible printed circuit (FPC) in a rectangular frame ("口" shape) pattern. As illustrated in Figure 7, this configuration guarantees a secure bond between the FPC and the SCF's copper foil after pad bending, effectively sealing a potential path for water infiltration from the FPC's underside.

Figure 6. Schematic diagram of FPC backside adhesive in the FOP state

After pad bending, a sealing and waterproof path for insulation tape attachment must be designed on the FPC and panel. This waterproof path, shown as the blue "trapezoidal" path in Figure 7, covers the vast majority of the FPC area, including the component area, and also covers the COP location on the panel. The bottommost part of the waterproof path is adjacent to the apex of the pad bend. Special attention must be paid to ensure that the waterproof adhesive near this location is not too close to the apex of the pad bend; otherwise, applying the insulation tape might crush the metal traces on the panel, causing functional failures such as display abnormalities. The insulation tape [3] is applied along this waterproof path, as schematically shown in Figure 7. When water contacts the FPC area, the sealed waterproof path formed by the insulation tape acts as the outermost waterproof barrier, preventing moisture from penetrating into areas such as components, FOP, and COP thereby avoiding electrical-related failures.

Figure 7. Trapezoidal waterproof path formed by insulation tape

3 .Experimental Validation

Characterization of Waterproof Performance for AMOLED Module Units: Research indicates that one of the highest waterproof ratings in the consumer electronics field is IPX8 [4]. Mobile phone manufacturers have extended this requirement to display suppliers for design and manufacturing. To simulate the IPX8 test conditions, the standard was deconstructed, revealing that it corresponds to submerging the device in 2 meters of water for 30 minutes without functional failure. Using the hydrostatic pressure formula p=mgh , the pressure at a 2 meter water depth is calculated to be 20 kpa. Based on this, the following waterproof test was designed:

P=mgh                                               （1）

H=pmg                                                                 （2）

Test Method:

- The module is connected to a test fixture, powered on, and immersed in water inside a testing apparatus.

- The pressure inside the testing apparatus is increased to 20 KPa via a pressure valve to simulate the conditions at a 2-meter water depth.

- The module remains powered on during the test, and any screen extinguishing is observed and recorded, along with the time of occurrence.

Table 2. Test Conditions for Pressurized Soak Testing Under Power

| Item | Content | Requirements |
| --- | --- | --- |
| 1 | Sample condition | Modules powered and illuminated |
| 2 | Pressure | 20kpa |
| 3 | Test duration | 30min，2hours，6 hours，8 hours |
| 4 | Test solution | H2O |
| 5 | Quantity tested | 10pcs |
| 6 | Schematic diagram of test setup |  |
| 7 | Test standard: | No failures allowed during the 2-hour test; touch functionality must remain operational post-test. |
| 8 | Results | Display-related abnormalities occurred in 3 modules within 2 hours. |

Failure Analysis: Dissection of Sample #3 revealed corrosion on a display-related capacitor. Compared to other capacitors, this specific capacitor exhibited incomplete and non-uniform conformal coating, which led to its electrochemical corrosion upon water exposure, as depicted in Figure 8.

FPC

Capacitor

Waterproof Adhesive

Incomplete and non-uniform conformal coating

(a) Partial view                             (b) Cross-sectional view

Figure 8. Capacitor corrosion

Analysis of the failed Samples #5 and #6 identified gaps in the FPC adhesive layer. As shown in Figure 9, during testing, water infiltrated through these gaps into the FPC gold finger area under atmospheric pressure, resulting in electrochemical corrosion and ultimately display failure.

Figure 9. Schematic diagram of FOP backside adhesive gap and resulting corrosion

Analysis Conclusion: The root cause of the failure was identified as localized absence of capacitor adhesive and the presence of gaps in the FOP back-side adhesive application. A secondary cause was the failure of the outermost waterproof path (insulation tape) and the FPC back adhesive path to effectively block water ingress under pressure. Further Analysis: The localized uneven adhesive application on the capacitor was analyzed to be due to clogging of the dispensing nozzle. The corrosion at the FOP location was attributed to gaps in the FOP back-side adhesive application [5], where the UV adhesive failed to form an effective waterproof barrier in the step coverage area after dispensing.

Improvement Actions: Countermeasure for Capacitor Adhesive Improvement: Regularly clean the adhesive valve and increase the frequency of automatic nozzle cleaning and wiping. Countermeasure for FOP Back Adhesive Gaps: Increasing the deposition width and height of the FOP backing adhesive, in conjunction with higher UV curing energy and longer exposure, effectively mitigated the problem, as illustrated in Figure 10.

Figure 10. Schematic diagram of the improved FOP adhesive application process

A subsequent problem to address is the elucidation of the waterproofing mechanism, which comprises the identification and characterization of the moisture barriers formed by the insulating tape and FPC adhesive. This constitutes a key research objective. To find the water ingress path through the outermost FPC insulation tape seal, methods are needed to characterize how water enters from around the FPC insulation tape and permeates into the FPC component area or the FOP back adhesive area. Through discussion and practical testing, the following test method was established: If water ingress paths exist between the module's FPC and the insulation tape, or between the FPC and the SCF, the finished module can be placed in a sealed pressure chamber filled with red ink for pressure testing. After a specified test duration, the module is removed, baked, and inspected to observe the red ink path, thereby identifying the water ingress route. Table 3 details the specific test conditions.

Table 3. Test Conditions for Red Ink Pressure Testing

| Item | Content | Requirements |
| --- | --- | --- |
| 1 | Sample condition | Modules unpowered and not illuminated |
| 2 | Pressure | 20kpa |
| 3 | Test duration | 2 hours |
| 4 | Test solution | Red ink or white ink |
| 5 | Quantity tested | 10pcs |
| 6 | Test equipment |  |
| 7 | Test Method | Immerse the finished module in red ink. Continuously pressurize the chamber via a pressure valve until the specified pressure is reached. After testing, bake the sample at 85°C for 5 hours. Following baking, disassemble the FPC layer by layer and examine the traces of red ink penetration. |
| 9 | Test Criteria | Pass (Optimal): No red ink penetration is observed in any laminate layers. Pass (Acceptable): Red ink traces are present, but without forming a continuous path through the adhesive seal. |

Testing of 10pcs modules revealed the following defects: After removing the insulation tape, red ink penetration paths were observed on the "trapezoidal" waterproof adhesive, and red ink residue was found in the component area and the DDIC area, as shown in Figure 10. When the module was unfolded into the FOP state, red ink traces remained on the spacer blocks and the FPC's rectangular (口-shaped) back adhesive, as shown in Figure 11. Analysis revealed that the FPC back adhesive width and the insulation tape's waterproof adhesive width were too narrow. Additionally, the contact area of the pressure head and the dwell time during pad bending and insulation tape application were insufficient, leading to inadequate adhesive activation.

(a) Removal of the insulating tape     (b) Deployment of the FOP

Figure 11. Results after red ink test showing the removed insulating tape and the deployed FOP

Improvement Validation Results: A Design of Experiments (DOE) was conducted using modules with the improved capacitor adhesive application and the recessed FOP back adhesive support film protective film. This DOE also involved widening the FPC back adhesive and the insulation tape waterproof adhesive, and increasing the dwell time. The red ink test results are shown in Table 4.

Table 4. Presents The DOE Verification Results.

| Plan | FPC backside adhesive Waterproof adhesive | FPC backside adhesive | Insulating tape | / |
| --- | --- | --- | --- | --- |
| Variables | Width increase | Dwell time |  | Test Results |
| DOE1 | Increased width ：1mm | Extend 3s | Extend 2s | 9pcs pass 1pcs fail |
| DOE2 |  | Extend 4s | Extend 3s | 10pcs pass |

Experimental Conclusion: Longer dwell time improves adhesive activation, leading to superior performance of the outermost waterproof barrier. This enhanced peripheral seal provides effective first-level protection for the internal electrical connection interfaces.

4. Conclusion

The waterproof performance of the AMOELD monolith module must achieve a rating of IPX8 or higher, necessitating improvements from both design and process perspectives. Based on our decomposition of the waterproof performance and the final experimental results, the following conclusions are drawn: First, it is essential to ensure optimal peripheral waterproofing, which includes the insulation tape, the waterproof path between the panel and FPC, the FPC back adhesive, the bonding integrity between the support film and spacer blocks, and the adhesive between the spacer blocks and SCF. Second, waterproofing at electrical connection points must be rigorously implemented, covering locations such as the FOP, DDIC, TP IC, and capacitive & resistive components. Two key factors influencing the waterproof performance of the monolith from design and process aspects are identified. The primary design influencing factors include:

- Adhesive width, thickness, and coverage area;

- Waterproof path design;

- Adhesive selection criteria (e.g., water absorption capacity, viscosity, hydrophobicity, anti-release properties, curing method, reliability performance, and chlorine content).

The process influencing factors are:

- Whether the back adhesive is fully activated, including dwell time, pressure magnitude, and contact area of the pressure head;

- UV adhesive application width, thickness, and the completeness of curing (UV wavelength, energy, duration);

- Potential defects in the adhesive layer post-lamination, such as bubbles, adhesive stretching, overflow, or insufficient adhesive at interfaces, as well as issues like lifting, openings, or wrinkling between laminated interfaces.

Experimental results demonstrate that a well-executed waterproof design combined with optimized module processing is critical to achieving superior module waterproof performance.

5. References

- Li, Y., Huang, J., and Qin, R. Screen Module, Mobile Terminal, and Screen Module Monolithic Coating Process, SID Digest, Vol. 54, No. 1, pp. 456-459, 2023.

- Zhang, H., Wang, L., and Chen, K. Display Module and Manufacturing Method Thereof, IDW Proceedings, Vol. 18, pp. 1023-1026, 2023.

- Xiao, S., and Li, R. Dustproof and Waterproof Design: The Sealing Structure and Air Tightness Detection Method of IPX8 Foldable Screens, 21st International Display Workshops, pp. 288-291, 2025.

- Kim, S., Park, J., and Lee, H. Advanced Sealing Structures for Foldable Phones with IPX8 Rating, SID Digest, Vol. 53, No. 1, pp. 321-325, 2022.

- Wang, X., and Li, Z. Partition Sealing Architecture and Material Innovation in Foldable Screen Phones, IDW Proceedings, Vol. 19, pp. 777-781, 2024.