A Study on the Anti-Electrostatic Field Performance of AMOLED Modules

Rukang Zhang*, Luna Wang**, Ying Cao**, Gaohui Xie**, Mingwei Ge**, Ying Shen**

*Guangzhou Govisionox Technology Co., Ltd. (Visionox's Affiliated Company), Guangzhou, Guangdong, China

**Guangzhou Govisionox Technology Co., Ltd. (Visionox's Affiliated Company), Guangzhou, Guangdong, China

Abstract

Based on customer complaints and user feedback from the market, electrostatic failures in AMOLED mobile display modules have evolved from early hard ESD damage to soft failures induced by frictional electrostatic fields, with symptoms such as green tint and green flickering. This paper begins by analyzing the failure scenarios and subsequently develops two testing approaches: one involving electrostatic friction testing that closely simulates real-world user failure conditions, and another utilizing a high-voltage direct current electric field test for rapid excitation. The latter method proves instrumental in enhancing the anti-electrostatic field performance of OLED modules. Furthermore, the failure mechanism is investigated by examining the charge transfer pathways within the module under electrostatic fields, the endogenous electric field in the polyimide (PI) layer, and its impact on the electrical characteristics of the TFT back channel, specifically the threshold voltage (Vth) and subthreshold swing (SS.). Finally, based on the failure mechanism analysis, countermeasures are proposed, including the implementation of BSM shielding in the display panel, optimization of three-layer film properties, adjustment of the BPF (Back Plate film), increased impedance of the PI layer, and process improvements in module manufacturing.

Author Keywords

AMOLED; Electrostatic Field; TFT; Vth; BSM

- Introduction

The protection of AMOLED (Active-Matrix Organic Light-Emitting Diode) modules against electrostatic discharge (ESD) has evolved from guarding against transient discharges-such as the Human Body Model (HBM) and Machine Model (MM), which occur on nanosecond to picosecond timescales-to defending against sustained electrostatic fields. According to consumer feedback and market complaints, a growing number of electrostatic-related failure scenarios no longer involve instantaneous ESD [1] damage leading to permanent product failure. Instead, soft failures-recoverable malfunctions-are increasingly observed after the device has been exposed to an electrostatic field for a certain period. User feedback indicates that these failures occur predominantly in northern regions, especially during dry autumn and winter seasons. A necessary condition for such failures is that the mobile phone is placed in a clothing or trouser pocket while the user walks for some time. It can thus be inferred that these failures result from continuous exposure to frictional electrostatic effects. Typical symptoms include a green tint, green flickering, or localized bright spots. However, after the device remains idle for a period, the failure phenomena disappear, and normal function is restored. A comprehensive study, encompassing failure analysis, mechanistic understanding, corrective measures, and the design of a robust testing methodology, merits significant research attention.

- Investigation of Testing Method

As is well established, triboelectrification is a prerequisite for electrostatic generation, and the failure environment for the product is an electrostatic field formed by continuous friction. Based on this necessary condition, we have explored the following test method to identify a friction head capable of easily generating triboelectric charges on the Cover Glass (CG) surface of individual modules. After investigation, a conductive nanofiber cloth was selected to fabricate the friction head, referred to herein as the "Electrostatic Friction Head." The corresponding test is designated as the Electrostatic Friction Test. The detailed testing procedure is summarized in Table 1 below.

Table 1. Electrostatic Friction Test Protocol

| Test Environment | Temperature: 23±3℃, RH: 35%RH~65%RH |
| --- | --- |
| Test Equipment | Electrostatic Friction Test Equipment |
| Indenter Parameters | 100g, 100mm/s |
| Test Specimens | AOMOLED Module |
| Test Pattern | 255gray 100% luminance |
| Sample Size | 10pcs |
| Test Duration | 8H, 24H |

The conductive nanofiber tip continuously rubs against the CG surface. A schematic diagram of the friction process is shown in Figure 1(a), and the corresponding friction motion trajectory is illustrated in Figure 1(b). The motion path is inset 15 mm from the Active Area (AA) boundary.

(a) Friction setup schematic          (b) Resulting motion path

Figure 1. Electrostatic friction mechanism and resultant trajectory

For early unimproved modules displaying the L255 pattern, the initial state observed before testing is shown in Figure 2. After exposure to the electrostatic field test, various display anomalies emerged at low brightness and low grayscale levels, including edge brightening with a greenish tint, progressive overall greenish display, localized bright spots, and green flickering, as depicted in Figure 2.

(a)Pre-test condition           (b) Observed defects after testing

Figure 2. Electrostatic friction mechanism and resultant trajectory

Extensive testing revealed that while this experimental protocol closely replicates real-world user scenarios, it suffers from several drawbacks: extended testing duration, low frictional voltage (with the maximum peak frictional voltage absolute value < 600 V), and a prolonged failure activation period (requiring up to 24 hours). To rapidly induce these defects and shorten the test cycle, it is necessary to develop a more efficient testing method. The core accelerating factor for this failure mechanism is the frictional electrostatic voltage. By focusing our research on this key influencing factor, we can enhance the acceleration efficiency and reduce the overall testing time. Based on this core factor, the overall test setup was designed as illustrated in Figure 3. The specific implementation is as follows:

- A high-voltage DC excitation power supply capable of outputting 0 to -6 kV is required.

- A display driving system is needed to simultaneously activate two OLED modules.

- Several pieces of conductive cloth and wires are utilized.

- The conductive cloth is attached to the cover glass (CG) surface of the module, inset by 15 mm from the active area (AA) boundary. Care must be taken to ensure the conductive cloth does not contact the ink edge of the CG to prevent short circuits between the positive and negative electrodes, which could cause electric shock.

- One wire connects the conductive cloth on the CG surface of both modules, and another wire connects the copper foil surface of both modules, establishing a parallel connection.

- The negative terminal of the DC power supply is connected to the conductive cloth on the CG, and the positive terminal is connected to the copper foil surface of the module.

Figure 3. Schematic diagram of the high-voltage DC excitation test

Following the establishment of the test setup according to this experimental model, extensive testing revealed that modules which typically failed within 8~24 hours under the conventional electrostatic friction test could be induced to exhibit the same types of defects in less than 2 hours using the high-voltage DC excitation method at -4 kV.

- Failure Mechanism Analysis

Based on failure analysis of defective units, it is hypothesized that the charge accumulation and transfer pathway within the module under an electrostatic field follows the model illustrated in Figure 4.

Figure 4. Pathway of charge accumulation and transfer under electrostatic field

Failure Path Inference: Electrostatically generated charges migrate from the Cover Glass (CG) surface along the ink edge to the module's cutting edge, then proceed to the edge of the supporting film beneath the display panel. The charges propagate from the edge across the entire surface of the supporting film. Charge accumulation within the supporting film affects the carriers in the TFT back channel, leading to alterations in the electrical characteristics of both the Driving TFT (DTFT) and Switching TFT (STFT), such as a positive shift in the Threshold Voltage (Vth) and an increase in the Subthreshold Swing (SS.). These changes induce display anomalies including edge brightening with a greenish tint, progressive overall greenish display, localized bright spots, and green flickering.

Within the electrostatic field, the presence of an endogenous electric field within the module is theorized, with the proposed conceptual model depicted in Figure 5.

Figure 5. Theoretical model of the endogenous electric field

The preliminary hypothesis suggests that after electrostatic injection, electrons accumulate on the surface of the backside supporting film and it’s adhesive. Mobile space charges exist within the Polyimide (PI) layer. Electron adsorption on the back surface of the PI layer prompts the rapid establishment of an internal electric field within the PI. Positive charges within the PI are attracted to the lower PI interface, while negative charges accumulate at the interface between the PI and buffer layer, thereby inducing positive charges in the back channel [3]. Due to the back channel effect, this influences the SS. and Vth of the TFT, ultimately leading to the electrostatic field-induced failure of the product.

Figure 6. TFT transfer characteristic curve

Explanation of the Failure Mechanism for Green Tint or Flickering:

Electrostatic friction generates negative charges, which transfer and accumulate between the PI layer and the supporting film. The electrostatic charges within the PI and supporting film impact the characteristics of both the DTFT and STFT, causing a positive Vth shift. As shown in Figure 6, which depicts the change in the TFT transfer characteristic curve before and after the test, a positive Vth shift results in a higher drain current (Ids) at the same gate-to-source voltage (Vgs). Given that the Green (G) sub-pixel possesses the highest luminous efficiency among the R, G, B pixels and is most sensitive to current variation, the ΔIds exerts the most significant impact on the G sub-pixel, leading to a dominant greenish display. Furthermore, a positive Vth shift of the TFTs in the Gate Driver on Panel (GIP) region causes the EM circuit to output extra pulses, consequently inducing screen flickering.

- Improvement Measures

Based on the product failure mechanism, improvements can be made to the polysilicon back channel of the TFT to stabilize its electrical characteristics. The countermeasures for the display panel are as follows:

- As shown in Figure 7, add a BSM (Back-Side Metal)[2] by depositing a metal Molybdenum (Mo) layer within the inorganic barrier or buffer layer (SiNx，SiOx) beneath the P-Si to shield the back channel. This can effectively reduce the impact of the endogenous electric field in the Polyimide (PI) layer on the electrical characteristic shift of the back channel. This shielding layer must be integrated into the inorganic barrier layer of the DTFT back channel within the Active Area (AA) to improve the greenish display at low brightness and low grayscale caused by DTFT electrical characteristic shifts. Integrating the shielding layer into the TFT back channel of the GIP area can mitigate the green flickering issue caused by extra pulse output from the EM circuit.

- Optimize the quality of the 3L film stack (collectively referred to as 3 Layer, consisting of SiNx, SiOx, and a-Si inorganic layers) by improving the process recipe for thin-film deposition, such as adjusting the power, and the flow ratios of SiH4 and NH3.

- Increase the impedance of organic adhesives like PI and BPF (Back Plate film) to weaken the influence of the endogenous electric field within the PI, thereby stabilizing the electrical characteristics of the TFT back channel and enhancing the module's resistance to electrostatic fields.

Module improvement countermeasures include:

- Applying conductive paste or silver paste on the module, as shown in Figure 8. The silver paste can be applied to the test side area of the OLED module to connect the Cover Glass (CG) and the copper foil. In real user scenarios, electrostatic charges generated by friction can be directly conducted from the CG surface to the copper foil of the SCF (composite tape), preventing charges from migrating into the supporting film and thus affecting the display panel.

- When performing integrated cutting of the module components including OCA, polarizer, panel, and BPF, the cutting parameters are optimized to increase the edge resistance of the module. This prevents charges on the CG surface from entering the display body along the cut edge.

Figure 7. Schematic diagram of TFT structure with electric field shielding layer

Figure 8. Schematic of the module structure with silver paste coating

After implementing the panel improvement measures, 10 modules were tested under the high-voltage excitation field test for 8 hours. No significant failure phenomena such as greenish display or green flickering were observed on any of the 10 modules under the Normal test image. Given the sensitivity of OLEDs to TFT current variations, especially at low brightness and low grayscale, the color coordinate shift of the 2nit-W32 pattern was measured before and after testing. The results are shown in Figure 9. After the 8-hour electric field test, the average CIE-y for 2nit-w32 was 0.325, with a maximum of 0.352. The objective color point showed a slight yellowish-green shift, but no subjective greenish display was visually perceived. This objectively demonstrates the effectiveness of the implemented countermeasures, proving their role in minimizing the impact of the electric field on TFT characteristic shifts.

Figure 9. Color coordinate shift of 2nit-w32 before and after electric field testing

- Conclusion

This paper investigated the anti-electrostatic field performance of AMOLED modules, covering testing methods, failure mechanisms, and improvement measures. A high-voltage DC excitation field test method was proposed to enhance testing efficiency and reduce test duration. The final characterization results of this method align with those of the conventional electrostatic friction test, while improving the failure excitation efficiency. Furthermore, the failure mechanisms behind the greenish display and flickering induced by the electrostatic field were explained. These are attributed to charge migration from the CG surface into the BPF during testing, leading to an endogenous electric field within the PI layer, which ultimately causes shifts in TFT parameters (Vth, SS.), resulting in failures. Based on the failure mechanism, several improvement strategies for both the panel and module were proposed. For the panel, incorporating a BSM within the inorganic barrier layer beneath the TFT can shield the electric field. Simultaneously, optimizing the deposition process of the 3L film stack enhances film quality. Increasing the impedance of materials like PI and BPF at the panel level is also effective. For the module, process improvements such as optimizing monolithic cutting parameters and applying silver paste can enhance anti-electrostatic field capability.

- References

- Duvvury C., Advanced Electrostatic Discharge Technology Issues, in Proc. CCE 2025, Mexico City, Mexico, Oct. 2025.

- Kim, J., Lee, S., and Park, H. A Study on the Optimization of Bottom Light-Shield for the Improvement of Negative Bias Illumination Stress Stability in Amorphous InGaZnO Thin-Film Transistors. SID Symposium Digest of Technical Papers, vol. 52, no. 1, 2021, pp. 556-559.

- Shen Y., Liu X., Guo  X., Zhang W., and Zhu X., P‐1.1: The Back‐channel Effect in Low Temperature Poly‐Si Thin Film Transistors, SID Symposium Digest of Technical Papers, 2024.