Failure Mechanism and Material System Collaborative Optimization of AMOLED Modules Under Back Impact

Yaling Wang, Ying Shen, Mingxing Liu, Fang Zhang, WeiLi, Xuelin Fan

Yungu (Gu'an) Technology Co., Ltd. (Visionox's Affiliated Company), China

Abstract

With the development of AMOLED display modules towards ultra-thinness in mobile terminals, their resistance to back impact has become a key bottleneck restricting product durability. This paper investigates the failure behavior of AMOLED modules under back impact loading. By combining experimental characterization and finite element simulation, it reveals that the failure mode is dominated by the fracture of the array substrate under tensile bending stress. Based on this mechanism, this paper proposes a collaborative optimization of the material system, emphasizing the synergistic mechanical response of multi-layer materials such as the backplane, cushion layer, and optical adhesive, and constructs an efficient energy absorption and stress dispersion system. Experimental verification shows that the optimized module improves its back impact resistance by 56%, providing an important theoretical basis and practical path for the development of highly reliable AMOLED display modules.

Author Keywords

AMOLED; Back Impact; Failure Mechanism; Finite Element Analysis; Collaborative Optimization; Material System

Introduction

With the market's pursuit of lightweight and ultra-high screen-to-body ratio in terminal devices, the structure of AMOLED display modules is developing towards being thinner and more integrated. However, while this complex structure enhances the visual experience, it also makes its mechanical reliability, especially impact resistance facing unprecedented severe challenges. Among them, back impact (i.e., impact from the direction of the device's back cover, such as dropping and squeezing) has become one of the main causes of screen failure (such as inner screen cracking, display abnormalities, bright or dark spots).Currently, research on the reliability of display screens mostly focuses on front impact or the strengthening technology of cover glass, and the optimal design of the collaborative working mechanism of multi-layer materials is a gap in the current research field. Systematically studying the failure mechanism of AMOLED modules under back impact and developing effective protection strategies based on this has urgent and important engineering significance for enhancing the core competitiveness of products.

Structure of AMOLED Module and Test

Structure of AMOLED Display Module：The main structure of the AMOLED display module from the front to the back is as follows in sequence: Cover Glass, OCA, POL, TP, TFE and OLED light-emitting unit, TFT array substrate, cushion layer, and metal backplane. The structural schematic diagram is shown in Figure 1.

Figure 1. Structural Diagram of the AMOLED Module

Design of Back Impact Experiment :  Before testing, all modules are placed in a standard temperature and humidity environment (23±2°C, 50±5% RH) for stabilization for more than 24 hours. For the dynamic impact test, a customized drop tower is used. The AMOLED module is placed on the loading platform, and a steel sphere with a specified size (R=7mm) and material is allowed to fall freely from a predetermined height to impact the back surface of the AMOLED display module, so as to simulate real drop conditions. Each condition is tested with 10 samples to ensure statistical validity. All modules need to be monitored for changes in display status after being impacted.

Failure Characterization: After the impact test, macroscopic and microscopic analyses are conducted on the failed modules. Macroscopically, there is no abnormality on the front appearance, while there are indentation traces of steel sphere drop on the metal of the backplane. After lighted, bright spots are found at the steel sphere drop position (Figure 2 a), accompanied by some dark spots, and no black spots or other defects are observed. To investigate the failure origin, the module with bright spots is selected, and SEM images clearly show that obvious micro cracks appear in brittle inorganic layers such as the gate insulating layer or interlayer dielectric layer in the TFT array region corresponding to the bright spots (as shown in Figure 2 b).

Figure 1. Macroscopic and Microscopic Image of bright spots

Failure Mechanism

Finite Element Simulation Model: In this study, a finite element model based on the explicit dynamics theory is established. The model strictly follows the layered structural characteristics of the AMOLED module. For the selection of material constitutive models, a differentiated modeling strategy is adopted according to the mechanical properties of different functional layers. The simulation model is shown in Figure 3 below.

Figure 3.  Simulation Model of Drop Ball Impact

Judgment and Discussion on Failure Mechanism: At the moment when the falling ball impacts the copper foil, a stress wave is generated. This stress wave propagates downward inside the module at the speed of sound. When the stress wave propagates to the bottom of the solid steel plate, due to the extremely high impedance of the steel plate, the stress wave will be strongly reflected, forming a reflected tensile wave that propagates upward. The reflected wave and the subsequent incident wave superimpose each other, resulting in a very high local stress peak (The moment when the maximum principal stress occurs is consistent with the moment of the maximum principal strain in Figure 4). When this peak strain exceeds fracture threshold (Maximum Principal Strain Theory (i.e., the Second Strength Theory) formula 3-1 and 3-2) of the inorganic layer, brittle fracture will occur directly and generate cracks. Cracks generally initiate from microscopic defects and propagate perpendicular to the direction of the principal stress.

Figure 4.  Curve of Changes of Various Variables

Figure 4 illustrates the curve of strain of the fragile layer during the falling impact process of the ball. It can be seen that the stress wave is gradually transmitted downward from the initial contact point of the falling ball until the stress wave rebounds at the bottom steel plate. Moreover, when the falling ball reaches the lowest point, the rebound force of the bottom fixture is the largest, and the strain of the fragile layer is also the largest.

εmax>εc        (3-1)

σ1−μσ2+σ3≤[σc]     (3-2)

As shown in Figure 2, in addition to the inorganic layer of the array, the general metal layer will also fracture. Although the TFT metal layer is ductile, its thickness is extremely thin, and it is also prone to fracture when wrapped and constrained by brittle inorganic layers.

Cracks cause the gate (M1, M2, GATO) or channel (Psi/IGZO) of one or more TFTs to break, making the data signal unable to be inputted. The gate voltage of the driving TFT is no longer modulated by the Data signal, and is stuck or drifts to a voltage value that makes it fully conductive. The driving TFT in a fully conductive state will generate the maximum current it can pass. This maximum and uncontrolled current continuously flows through the OLED, causing it to emit light continuously at the highest brightness.

Collaborative Optimization Design of Material System Based on Failure Mechanism

Optimization Objectives and Collaborative Design: Based on the failure mechanism, this study addresses the back impact issue of AMOLED modules and establishes a clear optimization objective: on the premise of maintaining existing optical performance, improve the impact resistance of the module by more than 50%. Specifically, the critical failure height in the drop ball impact test is increased from the existing 45mm to more than 67.5mm.

Aiming at the experimental mechanical conditions, collaborative optimization design of materials can be carried out from the following three aspects to reduce the stress on the array inorganic layer:

- Enhance energy dissipation above the failed film layer and set up multi-level energy absorption in the stress propagation path.

- Improve the elongation at break of the failed film layer.

- Improve the impedance matching below the failed film layer and reduce the local stress concentration caused by the superposition of impact incident waves and reflected waves due to impedance mismatch.

Selection and Optimization of Key Materials: According to Hertz Contact Theory (4-1), the contact radius a of a drop ball impacting a module is proportional to3FE∗. From the analysis of collision theory (4-3), when the equivalent modulus E∗ (4-2) increases, the overall stiffness k of the module increases. On the premise that the impact kinetic energy of the drop ball remains unchanged, the maximum deformation δ of the module decreases, the impact reaction force F increases, and the contact radius a increases. (See Table 1).

a=33FR4E∗      (4-1)

1E∗=1−v12E1+1−v22E2      (4-2)

F∝kδ=12δ2k∗2/δ   （4-3）

In addition to increasing the stiffness of the film above the failed film layer, the polymer chain structure, cross-linking density, and special fillers of the colloid above the failed film layer can also be adjusted to improve its loss factor and loss modulus under high-speed impact frequency, as shown in Figure 5. When silicone gel with a high loss factor (tan δ) is subjected to impact compression and shear, it can convert a large amount of impact kinetic energy into thermal energy through intermolecular friction, which means

That the energy transmitted to the fragile layers such as the lower metal and inorganic layers is effectively reduced. Based on this theoretical analysis, the impact resistance performance is optimally improved by 23% (base VS case5) by optimization of supporting film adhesive material after optimizing the supporting film material (see Figure6 and Table 1).

Figure 5. Chart of Loss Modulus and Loss Factor

Table 1. Module Material Optimization

| Material | Thickness(um) | Modulus (G Pa) | Material Selection | Strain (%) |
| --- | --- | --- | --- | --- |
| Cu | 18/25/35 | 88 | / | 1.6486/1.6312/1.6121 |
|  | 25 | 88/100/120 | / | 1.6312/1.6294/1.6247 |
| gel | 120/130/150 | / | base | 1.0115/1.0072/0.9503 |
|  | 120 | / | base/case1/case2/case3 | 1.0115/0.624/0.606/0.560 |
| BPF | 75/50 | 3.6 | / | 1.0115/1.0161 |
| BPF-PSA | 13/25 | / | base | 1.0115/0.9517 |
|  | 13 | / | base/case4/case5 | 1.0115/0.8387/0.779 |
| POL | 85/47 | / | / | 1.0115/1.1463 |
| POL-PSA | 20/15 | / | base | 1.0115/1.0281 |
| OCA | 150/100/75 | / | base | 1.0115/1.2438/1.3600 |
|  | 150 | / | base/case6/case7/case8 | 1.0115/1.120/1.116/1.114 |
| CG | 500/550/600 | 70 | base/case9/case10 | 1.0132/1.0115/1.0099 |

Figure 6. Simulation Comparison Chart of the Impact of Adhesive Materials on Impact Resistance Performance

After optimizing the adhesive material based on simulation, the back impact resistance of the module is significantly improved. Subsequently, impact absorption energy tests were conducted on the adhesive monomers, and the comparison results are shown in Figure 7. The impact energy absorption rate of the optimized adhesive material has increased by ~24.2%.

Figure 7. Comparison Chart of Impact Absorption Rate

Result

Based on the above theoretical analysis, the advantages of the optimized module stack are shown in Table 1. For the full-module AMOLED display module, the critical failure height of the back drop ball impact was 45mm before optimization, and it was increased to 70mm after optimization, with an improvement of 56%, significantly enhancing the back impact resistance of the full module.

Table2. Impact Resistance Performance Before and After Material Collaborative Optimization

| Item | Variable | Base | Superior Solution |
| --- | --- | --- | --- |
| Cu | Thickness | 25um | 25um |
|  | Modulus | 88GPa | 110Gpa |
| Gel | Thickness | 130 | 130um |
|  | Material | base | case3 |
| BPF | Thickness | 75um | 75um |
| BPF-PSA | Material | base | case5 |
| POL | Thickness | 47um | 47um |
| POL-PSA | Material | base | base |
| OCA | Thickness | 150um | 150um |
|  | Material | base | base |
| CG | Thickness | 550um | 550um |
| Ball Drop Failure Height（（mm） |  | 45mm | 70mm |

Conclusion

This paper investigates the failure mechanism of fragmented bright spots in AMOLED display modules under the back drop ball impact condition: the tensile strain on the backplane inorganic layer exceeds the material's own failure threshold, leading to local over-brightness caused by short circuits after fracture, which is macroscopically manifested as fragmented bright spots. After collaborative optimization of materials from the perspective of the entire module, the critical failure height of the back drop ball impact is increased from 45mm to 70mm, significantly improving the back impact resistance of AMOLED displays.

References

- Kim D, Lee S, Kim Y, et al. Dynamic mechanical characterization of flexible display modules under bending and impact for reliability assessment [J]. Journal of the Society for Information Display, 2021, 29(5): 364-375

- Ciavarella M, Hills D A, Monno G. The influence of rounded edges on indentation by flat punches [J]. Proceedings of the Institution of Mechanical Engineers, Part C: Journal of Mechanical Engineering Science, 1998, 212(4): 319-328