Super-hard dielectric Coating on Coverlens

Shenglin Lu*     Renjie liu*    guizhou Qiao*     Mingwei Ge*

* Product Engineering Center Department, Visionox Technology Inc. NO. 658,XiaDong Street, KunShan, JiangSu, Postal Code 215300, P.R.China

Abstract

The technology of Super-hard dielectric Coating on Cover lens Surface to enhance both hardness and scratch resistance, have attracted much attention now. In this work, through different types of material selection and optimization, different laminate designs optimization, we have developed multiple technical approaches which are planned application direction for smartwatch, mobile phone, tablet computer.

Author Keywords

Super-hard; dielectric coating; Si3N4; Cover lens; Diamond like Carbon(DLC); Mohs hardness; Friction resistance; Magnetron sputtering; Physical Vapor Deposition(PVD)

Introduction

Super-hard dielectric Coating technology，which by means of plating a layer of dielectric Coating on the glass cover lens with  magnetron sputtering process. Now different technical solutions have been developed，then it will be solved different technical issue.

With the Super-hard dielectric Coating，we can make sure that surface of glass cover lens Mohs hardness greater than 6，Steel wool friction >4200 times, eraser friction＞4200 times,  the water droplet angle after friction is greater than 90°.

| Item |  | Glass + AF | Glass + super hard coating + AF |
| --- | --- | --- | --- |
| Moh's hardness |  | 5 | 6 |
| Water contact angle |  | ＞110° | ＞110° |
| kinetic coefficient of friction |  | ＜0.04 | ＜0.04 |
| Steel wool friction | number of friction cycles | 3000 | 4200 |
|  | Water contact angle after friction | ＞100° | ＞100° |
| eraser friction | number of friction cycles | 3000 | 4200 |
|  | Water contact angle after friction | ＞100° | ＞100° |

According to Material selection differences and layered design solution, we mainly have three technical solutions which are Diamond like Carbon(DLC), Si3N4/SiO2, Si3N4/SiO2+DLC respectively, different technical solutions have different specification capabilities, and will applicate different directions.

Based on our plan,  Diamond like Carbon(DLC) solution will be used for smartwatch product and mobile phone products，then Si3N4/SiO2 solution will be used for smartwatch product and tablet computer.

| Layered design and thickness |  |  |
| --- | --- | --- |
| solution | Layered design | thickness |
| DLC | SiO-C-SiO-AF | 30nm-50nm |
| SiNO | SiO-SiN……SiO-AF | 200nm~2000nm |
| SiNO+DLC | SiO-SiN……SiO-C-SiO-AF | 200nm-400nm |

| Technology application target |  |
| --- | --- |
| solution | Planned application direction |
| DLC | Smartwatch and mobile phone |
| SiNO | Smartwatch and tablet computer |
| SiNO+DLC | Smartwatch and mobile phone |

Super-hard solution difference and discussion

2.1 Diamond like Carbon(DLC) solution

Diamond like Carbon (DLC) is the earliest developed process, the core of this solution is Carbon layer, which Determines the performance of the coating layer. In this scheme design, two layers of SiO2 sandwiching one layer of C, then plate Anti-Findgerprint layer at the outermost part of floor SiO2, which Plays a role in preventing water leakage.

| The laminated design of DLC |  |
| --- | --- |
| laminated material | thickness |
| AF | 5nm~15nm |
| SiO2 | 10nm~30nm |
| C | 3nm-10nm |
| SiO2 | 10nm-40nm |
| glass | 0.3mm-10mm |

The advantage of Diamond like Carbon (DLC) is thinner laminate Total thickness around 40nm; Processing time is short, coating time 60-90 minutes; Low white spot defect, Non-performing rate less than 10%; so it is Low processing cost solution.

Because of the thinner Coating layer, the shortcomings of Diamond like Carbon (DLC) are obvious. First, it is very difficult to control 5nm C layer design, Fluctuation in thickness leads to Hardness instability, Mohs hardness 6 test has poor stability. Secondly, due to the influence of the C layer, Diamond like Carbon (DLC) solution, Light transmittance is relatively low, the light transmittance is at a level of around 90%.

Reasons for achieving super hard of DLC is that the hardness of layer carbon is high，due to the stable chemical properties of carbon， the thicker the carbon -layer, the better the hardness capability. Now we have completed the DLC development and testing, here are the actual measured data of our sample and Transmission Electron Microscope (TEM) image

|  |  | sp1 | sp2 | sp3 | sp4 | sp5 |
| --- | --- | --- | --- | --- | --- | --- |
| transmittance (&550nm) |  | 90.1% | 89.9% | 89.8% | 90.2% | 89.9% |
| Moh's hardness |  | ＞6 | ＞6 | ＞6 | ＞6 | ＞6 |
| Steel wool friction | times | 4200 | 4200 | 4200 | 4200 | 4200 |
|  | Contact angle | 107° | 106° | 105° | 104° | 105° |
| eraser friction | times | 4200 | 4200 | 4200 | 4200 | 4200 |
|  | Contact angle | 110° | 109° | 109° | 111° | 108° |

2.2 SiNO solution

SiNO is the abbreviation for SiN/SiO layer. This solution is achieved through pure silicon magnetron sputtering excitation, and Excitation ionization of oxygen and nitrogen, then Generate SiN/SiO alternating stacks‌.

Through multiple layers of superposition, the thickness of SiNO solution can design range from 200nm to 3000 nm, when then thickness greater than 500nm, we can make sure that Mohs hardness 6 test stable, moreover ensure transmittance greater than 90%

| the laminated design of SiNO |  |
| --- | --- |
| laminated material | thickness |
| AF | 5nm~15nm |
| SiO2 | 50nm~100nm |
| S3iN4 | 60nm~150nm |
| SiO2 | 15nm~80nm |
| …… | according to thickness requirements |
| S3iN4 | 20nm~50nm |
| SiO2 | 10nm~30nm |
| glass | 0.3mm-10mm |

The advantage of SiNO solution is Excellent hardness performance, higher light transmittance. Disadvantage is that we need Longer time to Processing completed，that means we need Higher processing costs, Due to the long processing time, white spot defects have also significantly increased, in actual processing, the defect rate of white spots is around 20%.

In addition, Multilayer coating stacking causes large lab fluctuations, the fluctuation of a/b value reaches ± 0.2, moreover as thickness increases, a/b value fluctuations become larger.

Now  we have competed the SiNO solution development, and it will be used in our Different product types, and here are the actual measured data and Transmission Electron Microscope (TEM) image

|  |  | sp1 | sp2 | sp3 | sp4 | sp5 |
| --- | --- | --- | --- | --- | --- | --- |
| transmittance (&550nm) |  | 91.80% | 92.50% | 92.40% | 92.10% | 91.90% |
| Moh's hardness |  | ＞6 | ＞6 | ＞6 | ＞6 | ＞6 |
| Steel wool friction | times | 4200 | 4200 | 4200 | 4200 | 4200 |
|  | Contact angle | 108° | 111° | 109° | 106° | 108° |
| eraser friction | times | 4200 | 4200 | 4200 | 4200 | 4200 |
|  | Contact angle | 109° | 107° | 110° | 106° | 107° |

2.3 SiNO+DLC solution

In order to solve unstable hardness performance, poor light transmittance performance of  DLC solution, High white spot defect, Higher processing costs of SiNO solution, we developed SiNO+DLC combined solution， which can Synchronously solve the above problems.

The design method of SiNO+DLC is to Reduce the design total thickness of SiNO layers  to below 300nm， then plate a layer of C on the surface of the layer to enhance the hardness of SiNO.

| the laminated design of SiNO+DLC |  |  |
| --- | --- | --- |
| laminated material | thickness | design notes |
| AF | 5nm~15nm | Anti-Fingerprint |
| SiO2 | 10nm~30nm |  |
| C | 3nm~10nm | enhance hardness |
| SiO2 | 40nm~100nm | less than 300nm |
| S3iN4 | 70nm~120nm |  |
| SiO2 | 20nm~50nm |  |
| S3iN4 | 10nm~50nm |  |
| SiO2 | 20nm~50nm |  |
| glass | 0.3mm-10mm | baseplate |

The SiNO+DLC solution will avoid the issue of insufficient stability in the DLC solution, and avoid the issue of low yield in plan SiNO, It is expected to be a widely applicable technical solution

Application outlook‌ of Super-hard dielectric Coating

Scratches are the biggest problem with glass products， Super-hard dielectric Coating is a technology developed to enhance scratch resistance，now it can be used to small batches for smartwatch，mobile phone and tablet computer product.

With the increasing demand for scratch resistance quality, it will be applied to more and more product types，such as computer panel with AG effect，which To improve the anti-friction capability of the AG surface. It also be used to high-end ‌mobile phone‌ products.

According to the development and market demand is expected, we believe that the development and mass application of super-hard coatings are accelerating.

With the improvement of process capabilities, the yield of Super-hard dielectric Coating will be significantly improved, that will significantly reduce its processing costs, When the cost is low enough and most products are affordable, it will be widely used to various electronic products with glass covers.

Acknowledgments

This work was supported by super-hard coating development teams, who share the design, give the Technical Guidance.

References

- Research Status and Prospects of Super-hard multi-layer Thin Film. Construction Machinery School, chang’an University, 1001-3660(2005)03-0005-04

- Theoretial Study of MultiLayer Thermal Stress. Lanzhou Institute of Physics 1672-7126(2006)-0006-03

- Effect of spacer on the performance of the hydrophobic and hydrophobic property of the whole fluorine polyether. Hefei University of Technology 2016-06-11

- The research of super hard multilayer layers and Composite film.  Materials Science and Engineering of Jilin University 2005-01-17

- Nanomaterials for enhancing thin-film composite: design, fabrication, and application. Nanjing University of Science & Technology, Nanjing 210094