The Understanding and Improvement of Luminance Overshoot on Tandem OLED product

Xiaoning Liu*, Dawei Sun*, Hongyu Wang*, Chunliang Yao*, Liangliang Yu*, Yu Gao**,

Xin Teng*, Qiqi Ren*, Mengjing Zhu*, Shujuan Li*, Wonjun Song**

* Hefei Visionox Technology Co., Ltd., Hefei, Anhui, China

** Kunshan Govisionox Optoelectronics Co., Ltd. (Visionox’s Affiliated Company), Jiangsu, China

Abstract

In order to improve the instantaneous luminance overshoot while pattern switches at low gray scale on tandem OLED product, two new structure of tandem OLEDs were fabricated. The device characteristics slightly better than the conventional tandem OLED device. What's more, the luminance overshoot value reduces from 496% to 103% and 78% separately.

Author Keywords

Tandem; OLED; luminance overshoot; charge generation layer.

Introduction

Organic light emitting diode (OLED) has been a big interest of many people for next-generation future display for a long time. Tandem OLED is a stacked structure that connected with a charge generation layer (CGL) as the connection unit [1]. Due to their higher luminance and longer lifetime，tandem OLEDs have attracted widespread research and commercial interest over the past few decades [2-3]. It has gradually become the first choice for flagship products.

On tandem OLED product, the instantaneous luminance overshoot can be observed when pattern switches at low gray scale, such as from 2nit L0 to L32. For quantitative description this defect, luminance overshoot is defined as the maximum luminance of the first three frames divided by the steady state luminance. A typical phenomenon has been measured and shown in Figure 1. The luminance of the panel increase suddenly at the time of pattern switching, which is several times of the target luminance, and declines gradually at subsequent frame, then stabilizes at the target luminance gradually.

Figure 1. Luminance overshoot of tandem OLED

In this paper，a conventional tandem OLED device and two new structures of tandem OLED were fabricated. The characteristics of these devices such as Current density-Voltage (J-V), Capacitance-Voltage (C-V) and lifetime have been measured and discussed. Then these devices were applied on a mobile product, and the luminance overshoot have been measured by a C410. Finally, we try to make clear the mechanism of the overshoot phenomenon based on these results.

Experiment

As shown in Figure 2, three kinds of green tandem OLED devices have been fabricated. Device Ⅰ is a conventional structure that includes two OLED units connected by a charge generation layer (CGL). Device Ⅱ and Device Ⅲ are new structure which a functional layer is inserted just on the anode. The layer is named as capacitance optimization layer (COL).

Figure 2.  The schematic of OLED devices

These tandem devices were fabricated on ITO coated glass by G6 evaporation system. The current density-voltage (J-V) characteristics of the OLEDs were measured with a Keithley model 2602 power source. C-V measurements were performed by a LCR 6367 with a DC voltage range from 0 to 6V. A 75mV amplitude AC signal superimposed on the DC bias voltage was used to measure capacitance of these devices. The C-V measurement was measured at a frequency of 360Hz.

Result and Discussion

(a). J-V Characteristics: Figure 3 shows J-V characteristics of these tandem OLEDs fabricated (Devices Ⅰ, Ⅱ and Ⅲ). At a current density of 10 mA/cm2, the drive voltage of Device Ⅱ is almost the same with Device Ⅰ, and the drive voltage of Device Ⅲ is lower than that of Device Ⅰ by 0.2V (Table 1). Clearly, the drive voltage hasn’t deteriorative by inset a COL layer. It is noticed that the drive voltage of Device Ⅲ is lower than that of Device Ⅰ. This means that the COL2 is conducive to reducing hole injection barrier.

Figure 3.  J-V of Device Ⅰ, Ⅱ and Ⅲ

Table 1. J-V performance of Device Ⅰ, Ⅱ and Ⅲ

| Device | Von (V) | Vd (V) |
| --- | --- | --- |
| Ⅰ | 4.2 | 6.1 |
| Ⅱ | 4.2 | 6.1 |
| Ⅲ | 4.1 | 5.9 |

(b). C-V Measurement: These devices have been operated at current density of 4.5mA/cm2 in a temperature of 60℃ (HTO). After 96 hours of aging, C-V performance was measured again. Compared with the integral capacitance before HTO, all the devices have a little decline within 3%. As shown in Table 3. It’s indicated that they have similar capacitance stability.

Table 3. C-V performance of HTO

| Device | Before HTO | After HTO |
| --- | --- | --- |
| Ⅰ | 100.0% | 97.3% |
| Ⅱ | 100.0% | 97.0% |
| Ⅲ | 100.0% | 98.1% |

(c). Lifetime: Lifetime were measured at a fixed current density of 4.5mA/cm2 in the temperature of 25℃. The result is shown in Figure 4. The lifetime results of Device Ⅱ and Ⅲ are almost the same level with Device Ⅰ. What needs to be noted is the rise of voltage. The voltage increase is 0.06V of Device Ⅰ. Meanwhile, the voltage variation is decreased by 0.03V of Device Ⅱ and Ⅲ. This observation proved that the COL layer is beneficial to the stability of OLED device.

Figure 4.  Lifetime of Device Ⅰ, Ⅱ and Ⅲ, (a) Luminance, (b) Voltage

(d). Luminance Overshoot Measurement: A mobile product was fabricated using these devices and luminance overshoot was measured by C410 while the pattern switches from 2nit L0 to L32.

Figure 5.  Luminance overshoot of Device Ⅰ, Ⅱ and Ⅲ

As shown in Figure 5, there is an obvious luminance overshoot on panels using Device Ⅰ, the overshoot value is up to 496% and flicker is visible to the eye. Meanwhile, significant improvement can be obtained using Device Ⅱ and the overshoot reduces to 103%. In addition, luminance overshoot phenomenon nearly cannot be seen when pattern switches. Device Ⅲ exhibits the best performance among three devices and luminance overshoot has been completely improved.

Table 4. Luminance overshoot of Device Ⅰ, Ⅱ and Ⅲ

| Device | average | maximum | minimum |
| --- | --- | --- | --- |
| Ⅰ | 496% | 601% | 359% |
| Ⅱ | 103% | 118% | 84% |
| Ⅲ | 78% | 99% | 61% |

Discussion

Figure 6 shows the sectional view and drive schematic diagram of tandem OLED.

Figure 6.  Sectional view (a) and drive schematic diagram (b) of tandem OLED

CGL layer is evaporated with common mask. As a result, the OLED2 unit will extend to the pixel definition layer (PDL), which is rather different with OLED1. This will lead to discrepant carrier injection and capacitance between these two units. The capacitance of OLED2 is variable and affected by the horizontally conductivity of CGL. When pattern switches at low gray level, the capacitance of OLED2 is rather small, as a result luminance overshoot appears. With the horizontally mobility and accumulation of carriers within CGL layer, the capacitance of OLED2 increases and reach a stable value gradually, leading to the luminance decreases and stabilize consequently.

Conclusion and Outlook

The instantaneous luminance overshoot on tandem OLED affects the display quality of the product seriously. Although the defect can be improved partly by reducing the horizontally mobility of carrier in CGL layer. However, the performance of OLED device will deteriorate consequently. We have developed new structure of tandem OLED to improve the defect of luminance overshoot thoroughly. By inserting a COL layer, the differences of charge generation and horizontally mobility between two OLED units have been improved. As a result, the luminance overshoot improved.

References

- Tsukamoto Y, Shibasaki M, Nomiyama S et al. Highly Efficient Side -by-Side Three-Stack Tandem Flexible OLED Displays with Yb-doped n-CGLs: SID Symposium Digest of Technical Papers. 2024; 55:1070–1073.

- Shinya F, Toshiki S, Hiromi N et al. High-luminance and Highly Reliable Tandem OLED Display Including New Intermediate Connector Designed for Photolithography Applications: J Soc Inf Display. 2024; 32:309–319. Available from: http://wileyonlinelibrary.com/journal/jsid

- Tang J X, Fung M K, Lee C S et al. Interface studies of intermediate connectors and their roles in tandem OLEDs: J. Mater. Chem., 2010, 20, 2539–2548 | 2539.